## Slide 1: Application of High-Performance Computing and Machine Learning for Characterization of Nanostructures, Composite Materials, and Energy-Conversion Structures
Vasyl Kuryliuk and Oleg Olikh

## Slide 2: MD Simulations of Thermal Transport and Mechanical Behavior in Nanostructures and Composites

## Slide 3: Thermal Transport Modeling: Motivation and Objectives
(a) Growth rate of transistor count in processors (Moore’s law); (b) Historical trend of heat flux in bipolar and CMOS processors; (c) Computational efficiency vs. year and transistor length scale.

## Slide 4: Thermal Transport Modeling: Motivation and Objectives
Schematic of the various types of waste energy sources and utilization of waste heat energy by a thermoelectric generator. (Mater. Adv., 2021, 2, 1927-1956)

## Slide 5: Thermal Transport Modeling: Motivation and Objectives
Thermoelectric efficiency vs. hot-side temperature (Tc = 300 K). The 20–30% range marks the threshold for fossil-fuel replacement.
Figure of merit (ZT) vs. temperature for several typical thermoelectric materials.

## Slide 6: Atomistic Models for Thermal Transport Simulations

## Slide 7: MD Simulation of Thermal Conductivity
NEMD Method for Thermal Conductivity:
Divide the system into thin slabs along the heat flow direction.
Periodically swap velocities between the fastest atom in the cold slab and the slowest atom in the hot slab.
Repeated exchanges create a steady temperature gradient.
Compute heat flux and thermal conductivity from the resulting profile.

## Slide 8: MD Simulation of Thermal Conductivity
L1
L2
L3
Finite-size effects in thermal conductivity calculations using the NEMD method.

## Slide 9: MD Simulation of Thermal Conductivity
Time dependence of the heat flux autocorrelation function and its integral value.

## Slide 10: MD Simulation of Thermal Conductivity
Non-Equilibrium Molecular Dynamics (NEMD) Method | Equilibrium Molecular Dynamics (EMD) Method
Higher computational speed for the same number of atoms | Weak dependence of results on system size
Enables calculation of thermal boundary resistance between two materials | Allows calculation of thermal conductivity in all directions within a single simulation
Results depend on the system size | Lower computational speed
Thermal conductivity can be determined only along the imposed heat flow direction | Cannot determine thermal boundary resistance between two materials

## Slide 11: Computational Infrastructure
https://www.lammps.org
💎 Versatile molecular dynamics simulator: models solids, liquids, polymers, nanostructures, and biomolecules.
⚙ Supports a wide range of interatomic potentials — classical, reactive (ReaxFF), machine-learned (MLP), and hybrid quantum–classical (QM/MM) models.
⏩ Highly scalable performance — efficiently parallelized for thousands of CPU cores and GPU-enabled clusters.
🔬 Extensible and interoperable — integrates with VASP, Quantum ESPRESSO, ASE, Python interfaces, machine learning libraries, and data analysis tools.
Number of publications using LAMMPS by year

## Slide 12: Computational Infrastructure
Tools for Pre- and Post-Processing:
Tool for building, converting, and manipulating atomic structures for simulations
Script-based builder for complex molecular systems and LAMMPS input files
Generates initial atomic configurations by packing molecules without overlaps
Visualization and analysis software for atomistic simulation data

## Slide 13: SiGe Nanowires: Results and Analysis

## Slide 14: SiGe Nanowires: Results and Analysis

## Slide 15: SiGe Nanowires: Results and Analysis

## Slide 16: Phase-Change Composites

## Slide 17: Mechanical Behavior Modeling: Motivation and Objectives

## Slide 18: Mechanical Response and Crack Propagation

## Slide 19: Mechanical Response and Crack Propagation
ε=0%
ε=9.2%
ε=9.4%
ε=9.7%
ε=9.9%
ε=10.1%

## Slide 20: Mechanical Response and Crack Propagation
ε=0%
ε=9.5%
ε=9.6%
ε=9.7%
ε=13.8%
ε=14.0%

## Slide 21: Machine Learning for Thermal Conductivity
Symbolic Regression
approximates the relation between an input and an output through analytic mathematical formula
Interpretability
Physical content
Suitable for small data sets

## Slide 22: Machine Learning for Thermal Conductivity
Symbolic Regression
MD result:
SR result:

## Slide 23: Machine Learning for Thermal Conductivity
Symbolic Regression

## Slide 24: Machine Learning for Thermal Conductivity
Symbolic Regression

## Slide 25: Machine Learning for Carrier Mobility in Si
Symbolic Regression
models for mobility in silicon
Brooks & Herring
Conwell & Weisskopf
Fletcher
Caughey & Thomas
Dorkel
Masetti
Arora
Klaassen (Philips)
Noor Mohammad
…

## Slide 26: Machine Learning for Carrier Mobility in Si
Symbolic Regression
electron:
electron:
hole:
hole:

## Slide 27: Machine Learning for Carrier Mobility in Si
Symbolic Regression
electrons, majority carriers
holes, minority carriers
APE to Klaassen's theory

## Slide 28: Machine Learning for Carrier Mobility in Si
Symbolic Regression

## Slide 29: Machine Learning for Thermal Conductivity
GB, RF, SVR

## Slide 30: Machine Learning for Thermal Conductivity
GB, RF, SVR

## Slide 31: Machine Learning for Thermal Conductivity
Physics-Informed Neural Networks

## Slide 32: Machine Learning for Thermal Conductivity
PINN
Physics-informed convolutional encoder-decoder neural network maps

## Slide 33: Machine Learning for Thermal Conductivity
PINN

## Slide 34: Machine Learning for Thermal Conductivity

## Slide 35: ML Results and Validation

## Slide 36: Summary and Conclusions

## Slide 37: Future Work

## Slide 38: Acknowledgements

## Slide 39
Thank you
for your attention!