**Features of FeB pair dissociation and repairing in silicon n+–p-p+ structures under ultrasound loading condition**

Oleg Olikh1\*, Vitaliy Kostylyov2, Victor Vlasiuk2, Roman Korkishko2, Roman Chupryna1

*1Physics Faculty*, *Taras Shevchenko National University of Kyiv,Kyiv, Ukraine*

*2V. Lashkaryov Institute of Semiconductor Physics of NAS of Ukraine,Kyiv, Ukraine*

*\*E-mail address: olegolikh@knu.ua*

Abstract

The influence of ultrasound on iron--boron pair dissociation and association in silicon n+–p-p+ structures was investigated experimentally. The FeB pair transformations were monitored by measuring short circuit current kinetics. It was found that ultrasound causes the decrease both in concentration of pairs dissociated by light and time of association. The phenomenon was investigated at different light intensities, temperatures, frequencies and power of ultrasound loading. The possible mechanisms underlying the revealed effects were analyzed.

предлагаю такое резюме. Гладко и красиво ))

The experimental research in ultrasound impact on iron--boron pair dissociation and association in silicon n+–p-p+ structures has revealed the decrease in concentration of pairs dissociated by light, as well as in the time of pair associations.The experiments were performed at different light intensities, temperatures, frequencies and power of ultrasound loading. The FeB pair transformations were monitored by measuring short circuit current kinetics. The analysis of the revealed effects and their possible mechanisms show that ultrasound can be an effective tool for controlling silicon structure characteristics.

INTRODUCTION

It is of wide knowledge that the properties of semiconducting crystals and structures are determined very much by their impurity compositions. As a result, the methods aimed at modifying the system of defects are very important for practical applications. Most of these methods use irradiation, thermal treatment, or specific conditions of crystal growth. However, numerous experiments show that ultrasound also represents a sufficiently effective instrument to control the semiconductor defects. For example, it has been found that acoustic waves cause spatial redistribution of defects [], transformation of metastable point defects [], recharging of recombination centers [] and low temperature annealing of radiation defects []. The effects of this kind are observed in particular in silicon, which is the basic modern material used in microelectronics and solar power engineering [].

The advantages of using active ultrasound (US) are the local action of elastic oscillations and possibility to adjust the external impact by changing the type, polarization, or frequency of acoustic waves []. However, this method of modifying defect systems has not found wide application not least because of the lack of appropriate experimental research. In our opinion, it is most promising to use US loading (USL) as an additional factor of influence during various technological processes, which causes, in particular, the transformations in the defect system. This assumption is supported by the results obtained during ion implantation performed in the US field.

Iron is an important impurity in silicon-based integrated circuit and solar cell technology. Most often, iron-related defects are the main recombination centers that determine the lifetime of minority charge carriers in particular and device characteristics in general. Therefore, the methods aimed at iron gettering at various stocks have practical importance. There are quite many reports concerning defects of this kind. It is known that in thermal equilibrium at room temperature, virtually all Fe is present as FeiBs pairs in Si:B []. FeB pair dissociation can be accomplished by illumination at room temperature, by minority carrier injection, or by increasing the temperature []. Moreover, ultrasound vibrations with the frequency of 25-80 kHz and acoustic lattice strain of 10^-5-10^-4 (Cz—Si []) or 10^-6-10^-5 (poly--Si []) are capable of destroying FeB pairs. In practice, however, the most widely used technique is light-induced dissociation. The peculiarities of the dissociation and subsequent repair are well studied []. However, to the best of our knowledge, there are no reports about the US impact on these processes.

Our aim was to study experimentally the influence of ultrasound loading on the processes of FeB↔Fei+B\_s transformations in silicon solar cells (SCs). We used US with the frequency 2-30 MHz and strain <210^-6 . In order to prevent irreversible changes in the material properties, we used subthreshold intensity. The obtained results can be applied for subtle acoustically controlled tuning of the processes involved in iron atom gettering.

EXPERIMENTAL AND CALCULATION DETAILS

The n+-p-p+-Si samples used in the experiment are shown in Fig.1. The structure was fabricated from a 380 mm thick p-type boron-doped Czochralski silicon wafer with [100] orientation and resistivity of 10 Ohm cm. The n^+ emitter with surface resistance of about 20-30 Om and thickness of 0.7 mm was formed by phosphorus diffusion from the gas phase (POCl3) at 940 C. The anti-recombination isotype barrier was created by using p^+ layer (10-20 Om, 0.6 mm) formed by boron diffusion from the gas phase (BCl3) at 985C. On the front surface, the antireflective and passivating SiO\_2 (40 nm) and Si3N4 (30 nm) layers were formed. The solid and grid Al contacts were formed by magnetron sputtering on the rear and front surfaces respectively.

It has been found that some SC lots have significantly worse parameters compared to typical solar cells for this process. Additional experiments with thermal annealing at temperatures of 200C and 90C (the procedure is described by Tayyib []) showed that a sharp drop in the photoconversion parameters value is caused by iron impurities available in the SC base at concentrations up to 410^13 cm-3 in the SC base. It has also been found that the source of iron impurity is insufficiently pure chemicals that were used in the technological process for some SC lots. To study the effect of ultrasonic loading on the transformation of iron-boron pairs, the samples from these ``bad'' lots with various degrees of iron contamination ((0.2-4)10^13 cm-3) were taken. The area of the samples used in the experiment was 52×1.535 cm2.

To dissociate FeB pairs, the frontal side of the sample was illuminated with a halogen lamp with radiation intensity Will of 0.08-0.20 W/cm2. The illumination time t\_ill was up to 30 s.

The FeB pair association was monitored by measuring the kinetics of short circuit current ISC(t) after illumination by a halogen lamp –-- see Fig.2. ISC was measured under SC illumination by a low--intensity monochromatic light source (light--emitting diode SN--HPIR940nm--1W with light wavelength lambda=940 nm). The excess carrier density DeltaN induced by the LED illumination was estimated by using open-circuit voltage value according to Sachenko []. The DeltaN value (<10^12 cm{-3}) and duty cycle while ISC(t) measuring (0.5%) evidence that LED illumination is weak and does not cause FeB dissociation.

After illumination by the halogen lamp is terminated, FeB pairs are formed again and the starting value of ISC is completely recovered.

In fact, in conditions of homogeneous carrier generation in the base, which is several minority carrier diffusion lengths L\_n, the short circuit current can be described as follows []:

(1)

where alpha\_{ph} is the coefficient of light absorption, P\_{ph} is the light power, R\_{ph} is the coefficient of reflection, beta is the coefficient of quantum yield, mu\_n is the electron mobility, tau is the minority carrier lifetime in the base. In the assumption that it is the iron--related defects that play an essential role in the recombination, the following expression can be used to estimate tau:

(2)

Where tau\_i is the lifetime associated with intrinsic recombination, tau\_{SRH} and tau\_{SRH} are related to the recombinations at interstitial iron atoms Fe\_i and at FeB pairs, accordingly; tau\_{other} describes further recombination channels (other impurities, lattice defects, surface recombination). In order to calculate tau\_{SRH} and tau\_{SRH}, Shockley--Read--Hall model was used

(3)

Where N\_A is the material’s doping level (1.410^15 cm{-3}), n\_0 is the equilibrium electron concentration given by the law of mass action; n\_1 and p\_1 are given by

(4)

where E\_C and E\_V are the energies of the conduction band and valence band edge, respectively, N\_C and N\_V are the densities of states in the conduction band and valence band, respectively, and E\_t is the energy level of the relevant defect. The respective capture time constants of electrons and holes at the defect are given by

(5)

where N\_{Fe}(t) and N\_{FeB}(t) are the concentrations of Fe\_i and FeB, respectively, upsilon\_{th} is the thermal velocity, and sigma\_n and sigma\_p are the respective capture cross-sections of electrons and holes at the defect.

The time dependence of interstitial iron atom concentration after pair dissociation is described by the known expression from []:

(6)

where tau\_{ass} is the characteristic time of the complex association, according to []

(7)

where E\_m is the energy of Fe\_i migration; N\_{Fe,0} is the concentration of interstitial iron atoms formed due to illumination and N\_{Fe,eq} is the portion of interstitial iron atoms with N\_{Fe,0} that remain unpaired in equilibrium state. According to Wijaranakula [], N\_{Fe,eq} depends on temperature, doping level and N\_Fe,0}:

N\_{Fe,eq}= N\_{Fe,eq}(T, N\_A, N\_{Fe,0}). The estimations show that at 340 K N\_{Fe,eq}~0.1 N\_{Fe,0} for the samples under study.

In its turn, the iron--boron pair concentration N\_{FeB}, which is formed in the result of the partial association of N\_{Fe,0} can be estimated from

(8)

In case the intensive illumination causes dissociation of all the pairs, N\_{Fe,0} should be the same as the total concentration of the impurity irons in the structure N\_{Fe,tot}. If the duration (or intensity) of illumination is not sufficient for total dissociation, N\_{Fe,0}< N\_{Fe,tot}$. In the latter case tau\_{other} will also make contribution in the recombination of the FeB pairs that have not dissociated (with concentration N\_{Fe,tot}-N\_{Fe,0}-N\_{Fe,eq}(T, N\_A, N\_Fe,tot}-N\_{Fe,0})) as well as the respective number of Fe\_i (with concentration N\_{Fe,eq}(T, N\_A, N\_{Fe,tot}-N\_{Fe,0})).

In our calculations, we took beta=1, R\_{ph}=0.14 (the result of calculations according to Klyui []), mu\_n(T, N\_A) from Klaassen [], upsilon\_{th}^n and upsilon\_{th}^p from Green [], N\_C, N\_V from Couderc [], the defect parameters from Rougieux [], alpha\_{ph} from data []. In calculating tau\_i, band-to-band radiation recombination and Auger recombination were taken into account, and the temperature dependence of the corresponding coefficients was calculated according to Nguyen [] and Altermatt []. We used Eqs. (1)-(9) to fit the experimental data I\_{SC}(t). As fitting parameters P\_{ph}, tau\_{other}, N\_{Fe,0}, and E\_m were taken. The fittings were performed by using the metaheuristic method EBLSHADE [].

The example of fitting results is shown in Fig. 2. In our case, the parameters determined by fitting had the following values. P\_{ph} = 3.6 W which agrees well with the value measured by PowerMeter Rk-5720 (3.5 W). tau\_{other}>100 s, which testifies that the contribution of other recombination pathways can be neglected. N\_{Fe,0}=1.6 cm{-3}, which is close to the value obtained for the samples of the same series from L\_n measuring before and after intense illumination (0.5 cm{-3}). In this case L\_{n} was measured using spectral dependences of short circuit current [], the iron concentration was determined by using Zoth and Bergholz [] equation. Finally, E\_m = 0.655 eV. This value coincides with that well known from [], which is 0.66 eV. The coincidence of the values obtained by approximation with those obtained from other sources (first of all, E\_m value) proves that the investigations of I\_{SC}(t) after intensive illumination can be applied for estimating the parameters of iron-related defects. Moreover, the peculiarities of pair dissociation (see Sec.~2) found in this way also correspond to those reported in the previous publications, which testifies that this approach is quite appropriate. In fact, the time of I\_{SC} recovering is an indicator of how large the energy of migration is, and the amplitude with which I\_{SC} changes in the result of intensive illumination is associated with the concentration of iron atoms released in the process. It should be also noted that this approach is similar to the method proposed by Herlufsen [], in which actual concentrations of FeB pairs are estimated by the photoluminescence signal kinetics during pair association.

The measurements were carried out over a temperature range of 300-340 K. The temperature was varied by a thermoelectric cooler controlled by STS-21 sensor and stabilized by a computer-controlled PID loop.

In case of USL, the transverse (with frequency f\_{US}=0.3 MHz) or longitudinal (2-31 MHz) acoustic waves (AWs) were applied to the samples by using the piezoelectric transducer. The US intensities W\_{US} and amplitudes of strain xi\_{US}=\sqrt{2W/rho} (rho\_Si}=2.33 g/cm^3 is the silicon density, vartheta\_{US} is the US velocity, 9850 m/s and 5840 m/s (in cases of longitudinal and transverse AWs, respectively) does not overcome 1.3 W/cm2 and 210^{-6}, respectively. Since the focus of our research was the influence of elastic vibrations on FeB pair transformations, to avoid the effect of the piezoelectric field, the transducer was shielded --– see inset in Fig.2.

Results and discussion

FeB dissociation

In our investigation of light--induced FeB pair dissociation processes, we illuminated the structure with a halogen lamp varying the time of illumination t\_ill and afterward measured the kinetics of short circuit current recovery –-- see Fig.3. As seen from the figure, the time of short circuit current recovery does not change while the amplitude of light-induced changes depends on the time of illumination. Further approximation of the experimental curves by using the approach described in the previous section allowed us to estimate the number of pairs that dissociated in the result of illumination N\_{Fe,0} as a function of t\_{ill}. The experiments were carried out on a series of samples at different light intensities and temperatures in conditions with and without US loading. The typical results are given in Fig.3.

The obtained results show that as the illumination time grows the values of N\_{Fe,0} increase gradually until reaching saturation. This is in complete correspondence with the results of the previous researches [] that predict the exponential decrease of pair concentration with the increase of illumination time. The saturation should correspond to the condition of complete pair dissociation. The experimentally obtained dependences were approximated by using the following equation

(10)

Where tau\_{dis} is the characteristic time of dissociation, N\_Fe,fit} is the value corresponding to saturation. The examples of approximation curves are given in Fig.3, and the values of the parameters obtained by approximation --- in Table 1.

The other way to determine the equilibrium between free Fe\_i and Fe\_iB\_s is by using the following rate equations

(11)

where R\_a and R\_d are the association and dissociation rates of FeB pairs, respectively. From Eq. (10), taking into account that N\_{Fe}=N\_{Fe,tot}-N\_{FeB} and N\_{Fe}(t\_{ill}=0)=N\_{Fe,eq}, the time dependent interstitial iron content during illumination can be described as follows

(12)

The comparison of Eqs. (10) and (11) shows that tau\_{dis}=R\_a+R\_d, N\_{Fe,fit}=N\_{Fe,tot}. It should be noted that in our case (see Sec.2) tau\_{ass}>>tau\_{dis} (without USL tau\_{ass}=700 s at 340 K and tau\_{ass}=13000 s at 300~K). Therefore, R\_d>>R\_a and tau\_{dis}=R\_d, N\_{Fe,fit}=N\_{Fe,tot}.

As for the case without USL, we should note the following. First, for every sample N\_{Fe,fit} remains constant and does not depend on illumination intensity and temperature --- see Table 1. This is quite expectable if we assume that in this case N\_{Fe,fit}=N\_{Fe,tot}. Second, the value of tau\_{dis} (the last column in Table 1) depends on W\_{ill} and T. It is well known [] that the dissociation rate of FeB pairs increases quadratically with increasing illumination intensity. In the insets in Fig. 2 the values of tau\_dis are plotted against W\_{ill}. The linearity of the obtained curves is in complete coincidence with the reported data and can serve as an additional proof of the suggested approach applicability in estimating iron-related defect parameters. Moreover, it is known [] that the dissociation time decreases approximately twice per 20C increase. In our experiment, tau\_{dis}=11 s for sample SC350-2 (Fig.2(b) and Table 1) at T=320 K and at 340 K, it comprised 4.3 s, which justifies the expectations.

Another reason why it is advisable to analyze I\_{SC} kinetics is the behavior of tau\_{other} observed in the experiments. In the case when tau\_{ill} corresponds to the values of N\_{Fe,0} close to saturation, the other recombination channels can be neglected (tau\_{other}> 100 ms). In the case when the values of tau\_{ill} are small, tau\_{other} changes in the range 10^{-6}-10^{-4} s and begins to increase as the illumination time increases. In terms of the proposed approximation, this indicates that some parts of FeB pairs have not dissociated and the value of tau\_{other} is related to recombination on iron-related defects that do not reconstruct when the sample is kept in darkness. In order to support this assumption the quantity tau\_{other} was estimated as follows

(12)

Where tau\_{SRH} and tau\_{SRH} were calculated by Eq. (5) for defect concentrations N\_{Fe}=N\_{Fe,eq} and N\_{FeB}= N\_{Fe,tot}, accordingly. It turned out that tau\_{other} and tau, obtained in the same conditions, are very close: the correlation coefficient equals to 0.98 (see Supplementary Material).

Paying our attention back to the impact of acoustic waves on the processes of light--induced dissociation of FeB pairs, the following should be noted. First, USL actually does not influence the magnitude of dissociation time: tau\_{dis} values in neighboring rows are similar in the error range for all the cases in Table 1. Second, some pairs do not dissociate under illumination in the USL case: N\_{Fe,fit}< N\_{Fe,fit}. How large the portion of these pairs is, depends on US intensity (see Figs. 5(a), Table 1, W\_{ill}=0.16 W/cm^2); and at maximum W\_{US} values this portion reaches 10%. It should be noted that this [effect] is observed only in the case when light--induced pair dissociation is close to saturation. If W\_{ill} (or temperature), however, is that at which a part of iron atoms stays near the substitutional boron atoms at the given illumination times, then N\_{Fe,fit}=N\_{Fe,fit}.

FeB association

It has also been found that USL accelerates FeB pair association, see Fig.5(b). As seen from the figure, the main result of ultrasound excitation in the structure is the decrease in time of short circuit current recovery. Since in approximating experimental dependencies I\_{SC}(t) we assumed that pre-exponential multiplier in Eq. (10) does not depend on USL (but relies only on the temperature and level of base doping), in order to find numerical characteristics of this effect, we used the change in migration energy E\_{US}, i.e., it was assumed that

(13)

where E\_{m,0} is the migration energy estimated without USL, DeltaE is the acoustically induced (AI) change in migration energy. It is seen from Fig.2(b) that DeltaE depends on acoustic wave intensity. Fig. 6 presents the dependences DeltaE=DeltaE(W\_{US}) at varied US frequencies and for the samples with different iron content (estimated by the dependencies similar to those given in Fig. 5 under USL). The presented data show that

- DeltaE shows a practically linear dependence on US intensity;

- Effectiveness of AI change in migration energy decreases as the US frequency increases; transverse waves, despite their low frequency, less strongly impact the processes of iron ion diffusion;

- the magnitude of AI effect practically does not depend on iron concentration;

- AI change in migration energy can be as high as 13 meV.

DeltaE has not been found to depend on illumination intensity.

The data presented in Fig. 6 were obtained at 340 K. With the decrease of temperature, the AI effect decreases - see Fig. 6. As seen from the figure, temperature dependencies of DeltaE are close to linear:

(14)

where temperature coefficient alpha\_{US} depends on US frequency (see inset in Fig.5), while DeltaE depends also on the US intensity.

Possible mechanisms of ultrasound influence

It is obvious that the analysis of the possible reasons of US impact should be based on the mechanisms of iron-related defect transformation. It is suggested that FeB pair dissociation is a two-staged process []. First, the electron capture process leads to Fe\_i neutralization, which removes the Coulombic attraction between Fe\_i and B\_s. Second, the electron capture results in the deposition of diffusion barrier energy and spatial dissociation of atoms. In the literature, two possibilities are discussed: the second capture, which leads to negative charge state (Fe\_i) and consequently to Coulombic repulsion of Fe\_iB\_s pair, and the second capture, which deposits the necessary Fe\_i0 migration energy after recombination with a hole. The second way is known [] as recombination-enhanced defect reaction (REDR) and is caused by a strong electron-lattice coupling at the defect.

As for the association, it happens due to Fe\_i field-assisted migration to B\_s. Therefore, a more detailed expression for tau\_{ass} takes the following form []:

(15)

where iron diffusivity D\_{Fe}=D\_{0}\exp(-E\_m/kT), and in the general case [] D\_{0,Fe}=beta nu a\_2 exp(deltaS/k), beta is a correlation factor, nu is an effective vibrational (attempt) frequency, a\_2 is a jump distance, deltaS is the migration entropy.

For non-piezoelectric materials, the main effect of acoustic waves is associated with the mechanical stresses they cause. It is reported [] about several stress-related mechanisms of impurity diffusivity variation. For instance, Aziz [] shows that due to static stresses sigma\_{stat} in the crystal, the impurity migration energy can decrease by DeltaE=sigma\_{stat}Vast, where Vast is the activation strain tensor. It is known\cited {Yost} that as US propagates through the crystal,

it causes static strain:

(16)

Where beta is the acoustic nonlinearity parameter, u\_{US}=frac is the amplitude of lattice atom displacements. Therefore, the effect should be linear with respect to the US intensity, which correlates with the experimental data. It is known [], however, that Vast=(0.01-0.2)Omega, where Omega is the atomic volume (~2 m3 for silicon), and the value of the multiplier depends on the kind of impurity. If we consider the propagation of longitudinal waves in direction [100] (beta=2.0003 is assumed [], sigma\_{stat}=c\_{11} u\_{stat}, c\_{11}=166 GPa), for W\_{US}=1 W/cm2 we shall obtain DeltaE=5 eV. Therefore, this mechanism cannot be the cause of the revealed effect.

According to the data [], the diffusion of impurities in US fields can occur due to elastic deformation. In particular, the energy of interaction between a single defect and the strain field is given by

(16)

where K is the bulk modulus (102 GPa for Si), Omega\_d is the variation of crystal volume, in the result of point defect formation, for interstitial defect [] Omega\_d=(1.7-2.2)Omega, xi is the lattice relative deformation by the acoustic wave. The estimation of maximum interaction for W\_{US}=1 W/cm^2 yields E\_{int}=0.1 meV. And although Baransky [] states that in case of clusters containing N\_t defects, a collective effect can be observed, when E\_{int}-> N\_t E\_{int}, in our opinion, this mechanism cannot be crucial in the effect of AI acceleration of FeB pair association revealed in our research.

In turn, the most probable cause of decrease in tau\_{ass} is the process of impurity interactions with nonequilibrium excitations of the crystal lattice described in Refs. 15, which results in the change in probability of diffusion transitions. According to Pavlovich [], the US influence is that it causes the increase of crystal effective temperature and effective decrease of ``polaron'' activation energy. The latter is related to the transfer of lattice deformation around the impurity during diffusion transition []. It should be noted that according to calculations [], this effect should depend linearly on US intensity and temperature, which correlates with experimentally found peculiarities of AI changes. In addition, according to Krevchik [], DeltaE~t\_s, where t\_s is phonon collision time, which can account for the revealed frequency dependence of the effect.

It should be noted that the iron boron pairs are found to dissociate [] due to ultrasound treatment. In our opinion, the reported herein and previous results have a lot in common. In fact, according to Ostapenko [], Fe\_i has to ``jump'' to the next nearest interstitial under ultrasound action; we state about the decrease in Fe\_i migration energy value as well as the enhance of Fe\_i diffusivity in case of ultrasound loading. Further, the efficiency of AI dissociation increases with the rise of temperature and decrease of AI tau\_{ass}. The difference in the action of ultrasound (the iron-boron pairs dissociation or the enhancing of pairing) is associated with the difference in the intensity of the acoustic influence. For instance, the researchers used acoustic strain xi=10^{-5}-10^{-4} was used [] to dissociate FeB pairs in Cz--Si. Furthermore, Ostapenko and Bell [] regarded the resonance condition of pair reorientation (first step of dissociation) and used 25-70 kHz. In our case, xi<210^{-6} and f\_{US}=2-30 MHz are deficient to effectively overcome the Coulombic attraction between Fe\_i and B\_. Additionally, the presented data show that the effectiveness of acoustically-induced change decreases as the ultrasound frequency increases. Besides, it should be noted that Ostapenko [] asserted that in the case of predominant dissociated pairs, the ultrasound treatment may promote the pairing reaction in contradistinction to the case of high fraction of paired irons. In our case, the predominant dissociation was realized by intense illumination, and then the ultrasound loading accelerated pairing. Thus, the reported results provided empirical evidence for the above mentioned prediction.

As far as dissociation is concerned, it is worth paying attention to the possible US impact on the processes of charge carrier capture. For instance, it is suggested [] that in conditions of USL the capture cross sections for complex defects should change because of the change in effective distance between the components. In particular, this effect is expected to be especially substantial for the complexes whose components have Omega\_d with opposite signs. This is what is observed for FeB (Omega\_d(Fe)>0, Omega\_d(B\_s)<0) and for this reason, the complex should be acoustically active in terms of charge carrier capture. However, in our opinion, the processes of AI changes in sigma\_{n(p)} should have influenced, first of all, the characteristic time of dissociation, but actually, the effects of this kind have not been revealed. AI increase of R\_a should decrease N\_{Fe,fit} (see Eqs. (9),(10)), however this effect is leveled by the essential difference between tau\_{dis} and tau\_{ass}. Therefore, probably because of this reason, the US produces the impact on the second stage of dissociation. On the one hand, Korotchenkov and Grimmeiss show [] that due to the change of impurity location concerning the surrounding atoms in silicon under USL, the activation thermal energy of the carrier captured by the defect is decreased (up to about 10 meV at US intensities commensurate to those in our experiments). A similar increase of electron emission in our case should decrease the equilibrium part of negatively charged Fe ions experiencing Coulombic repulsion with B\_s. On the other hand, it is shown [] that USL of low intensity makes some part of the FeB pairs get rearranged in a metastable configuration with a different (orthorhombic) symmetry, in which the distance between the components is greater. At the over threshold US intensities, the spatial separation of this kind results in complete pair dissociations []. For our case, however, the important thing is that the decrease in distance weakens the Coulombic repulsion. In addition, the decrease in the concentration of pairs, which dissociate under illumination in the USL case, can be associated with a partial acoustically-induced FeB dissociation. In fact, if some pairs were dissociated by ultrasound waves, which had been pre-excited in the sample with a high initial fraction of paired Fe, they can not be dissociated under illumination. The decrease in the temperature or photon quantity leads to reduction in the set of FeB which was modified by ultrasound, or in the set of FeB which was modified by the capture of light-induced electrons, respectively. The sets cease to overlap and N\_{Fe,fit}=N\_{Fe,fit} --- see Table 1. Finally, USL can be the cause of weakening the electron-lattice coupling at the defect as well as the REDR process as a whole.

Numerous publications, see for example Refs. 35,36, report that during such technological processes as temperature stimulated diffusion of dopants or the formation of an antireflection coating, iron atoms also undergo gettering. This is caused by Fe ions diffusion to various stocks.

When performed in the US field, these processes, as the obtained results suggest, should improve the gettering effectiveness because of the greater volume from which Fe ions could be piled at the stocks.

CONCLUSION

The experimental research of ultrasound impact on the processes of FeB pair transformation was carried out in silicon $n^+$-$p$-$p^+$ structures at near room temperatures. The investigation has revealed the acoustically driven decrease in the portion of FeB pairs that dissociate under the action of light as well as the decrease in Fe ion migration energies. The latter effect depends linearly on ultrasound intensity; the temperature decrease and ultrasound frequency increase reduce the acoustically induced change of migration energy. The analysis has shown that these phenomenons are caused by the interaction of impurities with nonequilibrium excitations of the crystal lattice, and acoustically driven attenuation of Coulombic repulsion, which is caused by the increase in distance between pair components and/or change in defects’ charge. Thus, ultrasound can be an effective tool for controlling silicon structure characteristics.