1) Novelty and Contribution: The idea of applying pre-trained CV models to wavelettransformed kinetic data is interesting and potentially generalizable. However, similar signal-to-image ML transformations exist in other domains. The manuscript should emphasize what new physical or methodological insight this work provides beyond prior Fourier/wavelet-based ML approaches.

We thank the Reviewer for this insightful comment. We agree that Fourier- and wavelet-based signal-to-image transformations have previously been used in other fields, and that our manuscript must more clearly emphasise what is physically and methodologically new in the present work. Specifically, our study provides three key contributions that go beyond prior Fourier/wavelet-based ML approaches:

a) Previous CV based PV studies focus almost exclusively on macroscopic image data (EL/PL images) and use CNNs directly on visually interpretable images. In contrast, our work applies CV transfer learning to kinetic traces of FeB pair dissociation - a microscopic, purely physical signature that is not an image by nature. To our knowledge, no prior work has converted ISC relaxation kinetics into wavelet spectrograms for the purpose of quantifying point defect (Fe) concentration.

b) earlier signal-to-image ML approaches (in PV and outside it) typically rely on Fourier/wavelet transforms to enhance visual patterns before CNN processing. Here, the wavelet transform plays a different functional role: it encodes the physics of FeB association kinetics into a 2D time-frequency representation whose multiscale structure aligns with the hierarchical filters in modern CV backbones. We show that CV models (EfficientNetB7, NASNetLarge) capture this physics-driven structure remarkably well, even with extremely small datasets (<30 curves), demonstrating a previously unreported synergy between defect-kinetics physics and CV feature hierarchies.

To make the novelty explicit, we inserted the following sentences into the Introduction: “Unlike previous Fourier- and wavelet-based ML approaches, which typically serve to enhance image data or provide handcrafted spectrogram features, the present work demonstrates that pretrained CV models can extract physically meaningful patterns from wavelet-encoded FeB dissociation kinetics. This establishes a new methodology for applying CV transfer learning to microscopic defect-related signals, enabling accurate impurity quantification from extremely small datasets and revealing physical inconsistencies between kinetic models and real devices”

2) Dataset Size and Overfitting Risk: The study relies on extremely small datasets (25 simulated and 28 experimental samples). Although data augmentation is performed, flipping or rotating spectrograms likely introduces redundant samples rather than independent data points. The near-perfect R2 values (0.996–0.999) strongly suggest overfitting. A robust cross-validation (e.g., k-fold or leave-one-out) with uncertainty quantification is needed.

We fully agree that the use of small datasets requires special attention to overfitting and that naïve augmentation (flips/rotations) does not create statistically independent samples. Below we clarify the methodological safeguards already used in the study, provide additional justification, and describe new analyses added to the revised manuscript.

1) Why the near-perfect R2 values do not indicate classical overfitting.

Although R2 ≈ 0.996 - 0.999 may appear suspicious, these values are obtained only on the training datasets consisting of smooth, noise-free kinetic curves generated by deterministic physical simulations. As noted in the manuscript, each ISC(t) trace is uniquely determined by the single parameter logNFe, so regression on synthetic data becomes close to an inversion of a 1-parameter function. Thus, very high R² on the simulated training set is an expected consequence of determinism, not overfitting.

More importantly: all reported performance claims are based on independent test sets: 10 simulated curves with NFe values excluded from training; 28 experimental samples never used in training the synthetic models; 8 held-out experimental samples for the experimental-model case. The R² values on these independent datasets are lower (0.97–0.996), which confirms that the model is not memorizing the data but captures genuine correlations.

3) Simulation–Experiment Gap: A major discrepancy is observed between simulated and experimental predictions, requiring a post-hoc quadratic correction. This implies that the CNN–regressor models primarily learn the synthetic data distribution rather than physical correlations. The authors should explore physics-based domain adaptation or partial fine-tuning using experimental data instead of empirical correction.

We fully agree that the discrepancy between models trained on synthetic data and real experimental measurements deserves careful discussion, and that physics-based strategies for bridging this gap are preferable to purely empirical corrections. Below we clarify (i) the physical origin of this discrepancy, (ii) why the CNN-regressor models do learn physically meaningful correlations rather than memorizing synthetic distributions, and (iii) what modifications were introduced in the revised manuscript.

(і) The need for quadratic post-hoc correction is not caused by the CNN–regressor learning synthetic artefacts.

Rather, as discussed in the manuscript, the gap arises because: FeB dissociation/association model involves parameters (Em, Eb, A, Az, EFei) whose literature values vary widely; many of these parameters are not constant across the device, especially in the space-charge region; however, simulations assume spatial invariance; real devices exhibit non-uniform Fe depth distributions and variations in base thickness, both known to strongly affect ISC(t), but these effects are not included in simulations; the experimental curves contain physical noise (thermal, optical, instrumental) that is absent in synthetic data. Together, these factors produce a systematic model-physics mismatch, making a shift between synthetic and experimental feature spaces unavoidable.

(ii) The CNN–regression models do capture physical correlations

We respectfully clarify that this is not the case, supported by several observations:

- Test predictions of NFe on real samples follow a linear trend in log–log scale with R2 ≈ 0.97-0.99 before correction. This demonstrates that the model correctly learns the physical ordering of Fe concentrations.

- This is precisely what one expects when the physical model uses slightly inaccurate parameter values: the shape of ISC(t) is captured, but the absolute kinetics time scale deviates.

- If the CV feature extractor were merely learning synthetic artefacts, retraining on experimental data would not converge.

Thus the CNN is not memorizing simulation-specific patterns; rather, the simulation generates a slightly biased but physically correct input–output mapping.

4) Physical Model Validation: The SCAPS-1D simulations use fixed FeB parameters (binding energy, migration energy, and pre-exponential factors). Yet, these parameters vary widely in literature (0.55–0.69 eV for migration energy). Without sensitivity analysis or error quantification, the generated synthetic dataset may not reflect realistic kinetics. Validation against first-principles or experimental benchmarks would strengthen the study.

We fully agree that FeB-related kinetic parameters (binding energy, migration energy, pre-exponential factors, and level positions) exhibit substantial variation across the literature. This variation can significantly influence the association time τass and, consequently, the ISC(t) kinetics. Addressing this concern indeed improves the physical credibility of the synthetic data.

The parameters used in the original manuscript (Em = 0.66 eV, Eb = 0.582 eV) correspond to the most commonly cited values in defect-physics literature (Kimerling, Macdonald, Bothe, Voronkov). These values are also used in standard FeB-dissociation modelling workflows, including numerous prior studies of Fe kinetics in silicon.

Thus, the goal of the synthetic dataset was to establish a baseline, physically interpretable mapping between NFe and ISC(t) dynamics, not to fully replicate the variability of real devices. However, we agree that real samples do not follow a single deterministic parameter choice; hence, addressing sensitivity is essential.

5) Статті, в яких точкові дефекти та методи машинного навчання, що не зміг завантажити:

1) https://doi.org/10.1016/j.solmat.2024.113123

2) https://doi.org/10.1007/s11664-023-10533-4

3) https://doi.org/10.1021/acs.jpclett.5c01139

6) Схожість статей SST та SolarEnergy (SE):

1) однакові речення: «I-V curve simulations were performed for a silicon n+-p-p+ structure using SCAPS-1D version 3.3.11.» (SST) та «I-V curve simulations were performed for a silicon n+-p-p+ structure using SCAPS 3.3.11.» (SE)

2) Ідентичність логіки інтерпретації похибок: "The MSE metric alone does not fully reflect the accuracy... therefore MAPE and MedAPE were adopted..." (SST) та «The MSE and MAPE are highly sensitive to even a few low-accuracy predictions... therefore MdAPE was introduced...»

3) пояснення метрик та їх формульне визначення в двох статях ідентичне

4) однакові речення: "A detailed description of the modeling approach, including the used temperature dependencies of silicon and defect parameters, is provided elsewhere.."

5) дублюються схожим чином експериментальні деталі: «The current–voltage characteristics and Isc kinetics were measured using a Keithley 2450 source meter. The light emitting diode SN–HPIR940nm–1W with light wavelength 940 nm and intensity of about 5 W/m2 was used as low-intensity monochromatic light source. The LED radiation intensity was stabilized by a W1209 thermostat and a power supply regulated by a circuit incorporating positive feedback and digital control» (SE), «Current–voltage curves and ISC kinetics were measured using a Keithley 2450 source meter. A 940 nm SN-HPIR940nm-1W LED (intensity 5 W/m2) was used as a monochromatic light source, and its output was stabilized by a W1209 thermostat and a feedback-controlled power supply» (SST)

6) дуже схожі формулювання: «We used the Optuna toolkit to optimize model param-eters, employing the TPE sampler and Hyperband pruner for efficient hyperparameter selection. Tables S1-S5 (Supplementary Material) pro-vide the tuned hyperparameters and their search ranges. It is worth noting that 5-fold cross-validation was employed during the model tuning process, with 20% of the train data used as the validation set to evaluate models trained on the remaining 80%. The chosen hyperparameter combinations are presented in Tables S6-S10.» (SE) та «Hyperparameter tuning was performed using the Optuna toolkit, employing a TPE sampler and Hyperband pruner to ensure efficient selection. The complete list of tuned hyperparameters and their respective search ranges is provided in Tables S1–S5 (Supplementary Material). Five-fold cross-validation was implemented

during model tuning, with 20% of the training data used as a validation set to evaluate models trained on the remaining 80%. The resulting optimal hyperparameter combinations are presented in Tables S6–S10.» (SST)